## Slide 1: Bachelor OF TECHNOLOGY IN civil ENGINEERING
Under Guidance of
Dr. Lini Dev K.
Assistant professor
Dept. of Civil Engg., NITP.
Presented by
Riya Vishwakarma 2103070
Satyam 2103106
Vishal Kumar 2103089
Aditya Prakash pal 2103101

## Slide 2
Project Topic
Experimental Analysis of Soil Strength Parameters using Red Mud

## Slide 3: Introduction
Rapid industrialization has produced massive amounts of solid and liquid industrial waste.
Agriculture has also led to waste that affects the environment and ultimately human beings.
In India, about 4.43 million tonnes of hazardous waste are generated annually and 9.173 billion tonnes globally.
An industrial waste called red mud (RM) is considered as strengthening agent in the project.

## Slide 4: Table of contents
Introduction
Results and Discussions
Conclusion

## Slide 5
Industrial Waste
leads to
Global warming
Methane gas
Land degradation
Surface water contamination
Sub-surface water contamination
Human health
Animal health
Soil health
EFFECTS OF INDUSTRIAL AND AGRICULTURAL WASTE

## Slide 6
Industrial Waste
can be used in
Recycling
Adsorbents
Construction
Bio based oil
APPLICATION OF INDUSTRIAL AND AGRICULTURAL WASTE

## Slide 7
Red Mud
  Red mud is a potentially valuable solid waste with a global deposit of 4BT.
  It is generated by extracting alumina from bauxite.
  Process includes Milling & desilication, Digestion & clarification, Precipitation and calcination.
  It is highly alkaline and toxic.
  Methods and research's for the use of RM.
  Chemical and acid treatments were made to make it more effective.

## Slide 8
Figure 1. Red Mud Lake (Al Circle)

## Slide 9: Figure 2. Graphical representation of the production, utilization and utilization rate of red mud (Wang,2021)

## Slide 10: Application of Red Mud
Figure 3. Various applications of red mud

## Slide 11: Sample Collection
Red mud is collected from HINDALCO Ind. Ltd., Muri, Jharkhand.
Soil is collected from PMCH, Patna, Bihar.

## Slide 12: Results and Discussions

## Slide 13: Particle Size Distribution Curve of red mud
Soil Type | Percentage
Gravel | 0 %
Sand | 29.35 %
Silt | 57.15 %
Clay | 13.5 %
Figure 4. Particle size Distribution curve of red mud
Chart: Particle Size Distribution curve
| 10 | 4.75 | 2.36 | 1.18 | 0.6 | 0.42499999999999999 | 0.3 | 0.15 | 7.5274530877474127E-2 | 5.4858969974704096E-2 | 3.9911687974571237E-2 | 2.8686726574860443E-2 | 2.1515178825684898E-2 | 1.5935392080886592E-2 | 1.1371898766232461E-2 | 8.061864142621682E-3 | 5.8006352873226372E-3 | 4.1712056258365248E-3 | 3.0063086700423606E-3 | 2.2790321288061717E-3 | 1.7320828747416999E-3
 | 100 | 100 | 99.856 | 97.866 | 94.402 | 89.974 | 87.178 | 80.662 | 70.6488 | 63.133 | 55.6171 | 51.1076 | 45.095 | 40.5855 | 37.5792 | 33.0697 | 27.057 | 21.0443 | 18.038 | 13.5285 | 10.52
 | 60 | 60
 | 0 | 60
10 | 30 | 30
 | 0 | 30
 | 10 | 10
 | 0 | 10

## Slide 14
PROPERTIES OF RED MUD COLLECTED FROM HINDALCO
Specific Gravity | 3.086
Liquid Limit (%) | 38.79
Plastic Limit (%) | 35.56
Free swell index (%) | 10%
pH | 11.38
Maximum Dry density, MDD (g/cc) | 2.078
OMC (%) | 33.05
Void Ratio, e | 0.485
Cu | 30.63
Cc | 0.615

## Slide 15: Particle Size Distribution Curve of Soil
Figure 7. Particle size Distribution curve of Soil
Soil Type | Percentage
Gravel | 0 %
Sand | 20.174 %
Silt | 31.87 %
Clay | 47.95 %
Chart: Particle Size Distribution Curve
| 10 | 1.9120000000000002E-2
A | 60 | 60
B | 0 | 60
 | 100 | 97.964 | 96.646 | 94.532 | 92.488 | 89.512 | 88.452 | 85.472 | 79.826 | 67.3955 | 64.0205 | 58.1053 | 56.413 | 54.7207 | 52.1902 | 51.3441 | 49.6598 | 48.8136 | 48.4783 | 47.1213 | 47.1213 | 47.1213

## Slide 16: Proctor Test of Soil
Chart: MDD - OMC Graph
| 15.03 | 16.420000000000002 | 18.3 | 20.21
1 | 1.827 | 1.848 | 1.856 | 1.782

## Slide 17: CBR Test of Soil
Chart: Stress vs Penetration graph
| 0 | 0.5 | 1 | 1.5 | 2 | 2.5 | 3 | 3.5 | 4 | 4.5 | 5 | 5.5 | 6 | 6.5 | 7 | 7.5 | 8 | 8.5 | 9 | 9.5 | 10 | 10.5 | 11 | 11.5 | 12 | 12.5
 | 0 | 0.20814 | 0.34199 | 0.43569 | 0.52939 | 0.62308 | 0.67662 | 0.74355 | 0.81717 | 0.86402 | 0.93094 | 0.98448 | 1.0313 | 1.0715 | 1.105 | 1.1585 | 1.2053 | 1.2321 | 1.279 | 1.3124 | 1.366 | 1.4061 | 1.4463 | 1.4797 | 1.5132 | 1.5467

## Slide 18: Triaxial Test of soil
Chart: Normal Stress (kPa)
failure envelope | 24 | 130
c | 24 kPa
ϕ | 11.48°

## Slide 19: Properties of Soil collected from PMCH
Specific Gravity | 2.43
Liquid Limit (%) | 35.95
Plastic Limit (%) | 22.72
Free swell index (%) | 10%
pH | 8.56
Maximum Dry density, MDD (g/cc) | 1.86
OMC (%) | 17.8
Void Ratio, e | 0.306
Type of Soil (USCS) | CL
UCS (kPa) | 166.6
Failure Strain (%) | 10.52

## Slide 20
Cohesion, c | 24 kPa
Angle of internal friction, ϕ | 11.48°
Compression Index, Cc | 0.16
Recompression Index, Cr | 0.022
Permeability, k | 1.1847 x 10-7
CBR (@ 2.5 mm Penetration) | 8.296 %
Cont.

## Slide 21: Properties of Mixes Containing Soil and Red Mud
Mixes | Composition | Specific Gravity, G | Liquid Limit, LL | MDD (g/cc) | OMC (%) | pH
Mix 1 | Soil + 15% RM | 2.512 | 35.4 | 1.756 | 19.14 | 9.99
Mix 2 | Soil + 20% RM | 2.585 | 34 | 1.804 | 14.3 | 10.22
Mix 3 | Soil + 25% RM | 2.6 | 32.4 | 1.782 | 17.15 | 10.32

## Slide 22: UCS of Mixes Containing Soil and Red Mud
 |  | Unconfined Compressive Strength (kPa) |  |  |  | 
 |  | Curing Period |  |  |  | 
Mixes | Composition | 1 Day | 7 Days | 14 Days | 28 Days | 56 Days
Soil | - | 166.6 | 166.6 | 166.6 | 166.6 | -
Mix 1 | Soil + 15% RM | 252.798 | 278.07 | 369.51 | 433.74 | -
Mix 2 | Soil + 20% RM | 414.29 | 432.65 | 667.94 | 865.01 | -
Mix 3 | Soil + 25% RM | 257.69 | 242.71 | 297.2 | 357.44 | -

## Slide 23: Variation of LIQUID LIMIT WITH Red Mud
Chart: Liquid limit vs Specific Gravity
| 2.5099999999999998 | 2.58 | 2.6
 | 35.4 | 34 | 32.4

## Slide 24: Variation of MDD and OMC with Red mud
Chart: Dry Density vs Moisture Content
| 16.978727230786674 | 18.464097982858178 | 19.145356407222231 | 20.506950122649222
15% RM | 1.647 | 1.7291 | 1.7565 | 1.7332
20% RM | 1.722 | 1.8003 | 1.7968 | 1.7925 | 1.7368
25% RM | 1.6292 | 1.7279 | 1.7798 | 1.7622 | 1.7099

## Slide 25: Variation of stress-strain graph of mix 2
Chart: Stress vs Strain Graph
| 0 | 0.3289473684210526 | 0.6578947368421052 | 0.98684210526315785 | 1.3157894736842104 | 1.6447368421052631 | 1.9736842105263157 | 2.3026315789473681 | 2.6315789473684208 | 2.9605263157894735 | 3.2894736842105261
7 Days | 0 | 60.3809 | 128.9605 | 214.2225 | 341.6173 | 400.0623 | 432.6583 | 431.2064 | 404.4748 | 369.516 | 351.5242
1 Day | 0 | 43.1292 | 120.3632 | 197.0847 | 256.213 | 331.9666 | 381.7573 | 414.2963 | 404.4748 | 386.3122 | 359.8938
14 Days | 0 | 69.0067 | 180.5447 | 282.7737 | 444.1025 | 536.2537 | 636.2622 | 667.9472 | 665.6982 | 545.8759 | 343.1545 | 300.2816
28 Days | 0 | 8.6258 | 68.7789 | 171.378 | 341.6173 | 476.67 | 653.2292 | 760.9525 | 834.2294 | 865.0034 | 820.2231 | 700.657 | 648.3896

## Slide 26: CONCLUSION
The specific gravity of the soil increased with the addition of red mud, enhancing the soil's overall density and strength characteristics.
The highest MDD was observed at a 20% red mud (RM) addition, indicating optimal compaction and strength at this percentage.
The least OMC was recorded at 20% RM addition, suggesting better water absorption and soil stabilization at this proportion.
The liquid limit decreased as the percentage of red mud increased, contributing to improved soil plasticity and reduced swelling potential.
The highest UCS value was achieved at 20% RM addition, with a 419% improvement compared to the natural soil, demonstrating superior strength and load-bearing capacity.
The addition of 20% red mud provided the best overall results, making it suitable for various applications such as brick manufacturing, and as a material for subgrade and subbase layers in road construction and other engineering works.

## Slide 27: Reference
IS 2720 , Indian Standard Methods of Tests for Soil.

## Slide 28: Thank you